# Building a Better Cell Lab 4-2

# General Outcome #2:  Describe devices used to convert electrical energy.

- Can I understand the use of different chemicals and design for electrical storage cells?

## Part A: Testing Electrolytes

### Problem:

Which of the suggested liquids is best for making an experimental cell?

Hypothesis: (If, then, because...)

_________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

### Materials:

Voltmeter

2 connecting wires

electrode holder and cup

carbon strip

zinc strip

Liquids: distilled water, tap water, salt water, sugar water, vinegar,

soap solution, dilute ammonia, dilute ammonium chloride

### Procedure:

- Place zinc and carbon strip into electrode holders.

- Get a sample of the solution from the front and place your metals into the solution.

- Using the connecting wires, connect the positive (red) post of the voltmeter to the carbon strip, and the negative (black) post of the voltmeter to the zinc strip.

- Record the voltage, if any, of your cell.

- Remove your metals and rinse off the ends.

- Return your solution sample and take another to test.

- Repeat for the other seven samples.

Observations Part A:

#### Drawing of Apparatus

| LIQUID USED | VOLTAGE OBSERVED (V) |
| --- | --- |
| 1. Distilled Water |  |
| 2. Tap Water |  |
| 3. Salt Water Solution |  |
| 4. Sugar Water Solution |  |
| 5. Vinegar |  |
| 6. Soap Solution |  |
| 7. Ammonia and Water Solution |  |
| 8. Ammonium Chloride Solution |  |

Conclusions Part A:  What liquid created the best experimental cell?  Include evidence to support your claim.  Include any possible sources of error.  Also include an application to real life science decisions.

______________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

# Part B: Testing Electrodes

### Problem:

What metal or combination of metals is best for making an experimental cell?

Hypothesis: (If, then, because...)

__________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

# Materials:

voltmeter

2 connecting wires

2 strips each of carbon (C), zinc (Zn), copper (Cu), nickel (Ni), aluminium (Al), iron (Fe), lead (Pb)

beaker of liquid (your best solution from part A)

# Procedure:

- Using the liquid that gave you the highest voltage in part A, start using carbon and zinc and record your voltage.

- Remove metals and rinse them under water.

- Try different combinations of metal strips and record combination and voltage for each test in observation sheet supplied (need to do 10 tests).

*for some tests, you may have to reverse the connections to the

voltmeter in order to get a reading

Observations Part B:

Solution used for each trial:  ________________________

| METALS USED | VOLTAGE OBSERVED (V) |
| --- | --- |
| 1. carbon with zinc |  |
| 2. with |  |
| 3. with |  |
| 4. with |  |
| 5. with |  |
| 6. with |  |
| 7. with |  |
| 8. with |  |
| 9. with |  |
| 10. with |  |

Conclusions Part B:  Which metals created the best experimental cell?  Include evidence to support your claim.  Include any possible sources of error.  Also include an application to real life science decisions.

______________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Analysis Questions:

- Which three liquids in Part A gave the highest voltmeter readings?

_______________________________________________________________________________________________________________________________________________________________________________________

- Which three pairs of metals in Part B gave the highest voltmeter readings?

_______________________________________________________________________________________________________________________________________________________________________________________

- What seems to have the most effect on the voltage of the cell: the liquid used or the combination of metals used?

____________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

- To ensure the tests were fair, what conditions had to be kept constant (controlled variables) in

  - Part A?

________________________________________________________________________________________________________________________________________________________________________

  - Part B?

________________________________________________________________________________________________________________________________________________________________________

- Create a rule for you to explain what will create the best type of wet cell.

____________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

# Text boxes

Name:  ________

Date:  ____________

Class:  ___________